SECTION 08 81 13

TITLE: Backpainted Glass

Backpainted Glass by Element Designs for vertical and horizontal surfaces

Display hidden notes to specifier by using "Preferences"/"Tools"/"Options"/"View"/"Hidden Text".

Element Designs Inc. – Custom& functional aluminum frame glass products

This section is based on products by Element Designs, which is located at:

235 Crompton Street

Charlotte, NC 28732

Toll Free: 877-32203396

Phone: 704-332-3114

Fax: 704-332-3267

Web: www.element-designs.com

E-mail: info@element-designs.com
 
Element Designs is the leading manufacturer of aluminum frame glass cabinet doors & illuminated aluminum frame LED panels.  All products are custom manufactured to the specifier's requirements.  Element Designs’ manufacturing plant is in Charlotte, NC and ships product throughout North America through a network of 100 dependable distributors.

- GENERAL

  - SECTION INCLUDES

A.  Backpainted colored glass, referred to as backpainted or backcoated glass

RELATED SECTIONS

* NOTE TO SPECIFIER* Delete any sections below not relevant to this project; add others as required

A. Section 08 81 13 – Decorative Glazing

  - REFERENCES

* NOTE TO SPECIFIER* Delete any sections below not relevant to this project; add others as required

A. ASTM International

1. ASTM C 1036 Specification for Flat Glass

2. ASTM C 1048 Specification for Heat-Treated Flat Glass

B. American National Standards Institute (ANSI)

1. ANSI Z97.1-2004 Glazing Materials Used in Building-Safety Performance Specifications and Methods of Test

C.  American Society of Civil Engineers (ASCE)

1. ASCE 7-98 Minimum Design Loads for Buildings and Other Structures

D.  Consumer Product Safety Standard (CPSC)

1. 16 CFR 1201: Safety Standards for Architectural Glazing Materials

E.  Glass Association of American (GANA)

1.  GANA Glazing Manual

2.  Bulletin 01-0300 – Proper Procedures for Cleaning Architectural Glass Products

  - SUBMITTALS

    - Submit under provisions of Section 01 33 00 for general submittal requirements

    - Manufacturer’s data sheets on product being used.

1.  Technical Manual

2.  Samples: Manufacture supplied samples of 4” x 4” or 12” x 12” of backpainted glass

  - QUALITY ASSURANCE

    - Element Designs’ employees are fully trained on the procedure for handling glass products and the technique to backpaint glass to meet and exceed industry standards

B.  Installer Qualifications: Glazing Professional

  - DELIVERY, STORAGE, AND HANDLING

    - Store products in manufacturer’s unopened packaging until ready for installation.

    - Store in dry, protected, well ventilated area and protect from damage.

  - PROJECT CONDITIONS

A. 	Maintain environmental conditional (temperature, humidity, and ventilation) within limits recommended by 	manufacturer for optimal results.  Do not install products under environmental conditions outside manufacturer’s 	absolute limits.

  - WARRANTY

A. Provide manufacturer’s one year warranty on backpainted glass products

- PRODUCTS

  - MANUFACTURER

A.  	Acceptable Manufacturer: Element Designs Inc., which is located at: 235 Crompton Street / PO Box 7747; 			Charlotte, NC 28273 / 28241; Toll Free Tel: 877-332-3396; Tel: 704-332-3114; Fax: 704-332-3267; Email: 			info@element-designs.com; Web: www.element-designs.com

** NOTE TO SPECIFIER **  Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

B.	Substitutions:  Not permitted.

C.	Requests for substitutions will be considered in accordance with provisions of Section 01600.

  - Backpainted Glass

    - Approved Product: Element Designs’ water based backpainted glass

Specifier notes on Element Designs backpainted glass:

      - Element Designs backpainted glass utilizes the highest quality industrially available water based paint designed for the specific application of coating glass panels.

      - All glass is optically clear low iron from Element Designs to achieve optical clarity (no jade color), consistency and performance.

      - All glass is tempered for strength, durability and safety.

      - Each backpainted color glass will have an additional light grey backer color for total opacity and increased durability.  Matching primary color over backer color is available upon request.

      - Maximum backpainted glass panel size is 120” x 48” for 6mm, 10mm and 12mm thickness.  4mm maximum backpainted glass panel size is 96” x 48”.

B.  Backpainted tempered glass by Element Designs on low iron PPG Starphire in various thickness and finishes:

** NOTE TO SPECIFIER **  Delete the PARAPAN Color & Code not required in project

a. 4mm (5/32”) gloss (smooth surfaces both sides)

b. 4mm (5/32”) matte (top surface satin etched)

c. 6mm (1/4”) gloss (smooth surfaces both sides)

d. 6mm (1/4”) matte (top surface acid etched)

e. 10mm (3/8”) gloss (smooth surfaces both sides)

f. 12mm (1/2”) gloss (smooth surfaces both sides)

g. 12mm (1/2”) matte (top surface satin etched)

Note:  Other low iron thicknesses and surface finishes may be available upon request

C. Edgework options on Element Designs backpainted glass:

a.  Flat edge polish (available in 4mm, 6mm, 10mm and 12mm thicknesses) – EXPOSED edge applications

b.  Seamed edge (available in 4mm, 6mm, 10mm and 12mm thicknesses) - CONSEALED edge applications.

D. Color options on Element Designs backpainted glass:

a.  Standard Colors:  selection of nine standard colors – see manufacturer’s website or catalog

b.  Non-Standard Colors:  selection of 277 pre-formulated RAL colors – see manufacturer’s website or catalog

c. Custom Colors:  Element Designs can match any paint supplier’s SOLID color code or by a physical color swatch.  Color samples on specified glass type, thickness and finish will be produced and approved prior to production.

PART 3   	 EXECUTION

  - EXAMINATION

A. 	Do not begin installation until all products are properly prepared by a glazing professional.

3.2      INSTALLATION

A.	 Install in accordance to manufacturer’s instructions / recommendations.

3.3	PROTECTION

- Protect installed product until completion of project.

END OF SECTION